CUSTOM FORMULATING & BLENDING, INC.

CFB

Industrial Oils and Greases

SPINDLE #22

ISO GRADE 22 SPINDLE OIL

PHYSICAL SPECIFICATIONS

- Color			1.5 max

- Odor         	     	characteristic

- Appearance		Clear, Liquid

- Viscosity  @     40C  	 CST  22.0

- 40 C 	 SUS 107

- A.P.I. Gravity 	  60F	  33.0 Typical

- Specific Gravity  60 F  0.8586 Typical

- Density (LBS/GAL)	  7.15

- Flash Point                     400F

- Pour Point              	   + 15F

SPINDLE #22 is highly refined paraffinic oil formulated with oxidation inhibitors to produce a product with excellent oxidation resistance.  Spindle Oil # 22 is a light colored lubricant designed for high-speed machine tool spindles.

The outstanding characteristics of this product coupled with the cost / performance function ratio justifies looking at replacing your present spindle oil.

To obtain samples and pricing information please contact any of our professional customer service representatives.

CFB., Inc.

17716 Commerce Drive

Bristol, IN 46507

Phone (574) 848-5288						 Fax      (574) 848-5963